## Slide 1: Simple Tutorial for VASP
Guozhen Zhang, Xijun Wang
(guozhen@ustc.edu.cn)
2016.11.24

## Slide 2: What VASP can offer?
structure( via optimization) and energy
electronic and magnetic structures
  (partial, local) density of states
  bands structure
  charge distributions (STM simulation)
  work function
  magnetism structures
ab initio molecular dynamics
vibrational frequency (IR)
reaction paths
core level shift (CLS)
Berry Phase, optic properties, etc
Notes: CLS – X-ray photoelectron spectroscopy spectra of surface atoms

## Slide 3: Computational Setup
Periodic boundary condition , supercell
Plane wave basis sets (ENCUT, ENAUG)
K-points sampling (Automatic, or manual)
Pseudo Potential: UltraSoft PP and PAW
LDA, GGA, hybrid functional
  PW91, PBE, RPBE
  PBE0, HSE06…
other strategy
  L(S)DA+U
  vdW-DF functional
  GW method
  ……

## Slide 4: How to Start a VASP Calculation?
An pre-compiled executable file of VASP
Four input files
  INCAR: control parameters
  POSCAR: lattice constant and coordinates of atoms
  KPOINTS: k-points sampling
  POTCAR: chosen pseudopotential
How to prepare input files?

## Slide 5: Basic Idea of SCF Calculation in VASP

## Slide 6: The INCAR File
Electronic Part
  SCF
Geometric Part
  Optimization/single point calculation
Rest
  VDW correction
  DOS calculation output control
  Print control (charge and wavefunction)
  parallelization
Keyword list and the details are available in the VASP manual.

## Slide 12: Are Our Results Physically Meaningful?

## Slide 16: How to Get a Valid Geometric Structure?
geometric optimization of lattice constants

## Slide 22: Important parameters
Accuracy: Medium, Accurate, High…
ENCUT: ***eV
ISPIN: =1 or 2 (closed shell or open shell)
ISMEAR: 0, 1, 2, -5….
SIGMA
IRION = -1, 0, 1, 2, 5, 6 ….
ISIF = 2, 3, 4….
ISYM = 0, 1, 2…
VOSKOWN = 1
EDIFF, EDIFFG,
NSW step
GGA = PW | PB | LM | 91 | PE | RP | PS | AM

## Slide 23: Advanced Properties
band structure
(partial, local) density of states
charge distribution (STM…)

## Slide 27: Band Gap (I)
L(S)DA+U (NiO, FeO….) eg:
LDAU = .TRUE.
LDAUTYPE = 1 # Dudarev's
LDAUL =-1 -1 -1 2 -1
LDAUU = 0 0 0 2.7 0
LDAUJ = 0 0 0 1.0 0
PRB 71, 024502 (2005)

## Slide 28: Band Gap (II)
PBE0 (CO) GGA= PBE0
JACS 129, 10402(2007)
# Exchange and Correlation functionals
AEXX =0.25
AGGAX =0.75
AGGAC =1.0
ALDAC =1.0
ENCUTFOCK= 0
LMAXFOCK = 4
NKRED = 2
TIME = 0.4
LHFCALC =.TRUE.

## Slide 29
HSE06 (semiconductor)
# Exchange correlation treatment:
LHFCALC = .TRUE.
HFSCREEN = 0.2
AEXX = 0.25
AGGAX = 0.75
ALDAC = 1.0
AGGAc = 1.0
ENCUTFOCK= 0
LMAXFOCK= 4
NKRED = 2
TIME = 0.4
JACS (2012)

## Slide 34
Analysis of molecular orbital

## Slide 35: Electron Localization Function
LELF = .TRUE. | .FALSE.
ELFCAR
Nature 371 (1994) 683-686
Angew. Chem. Int. Ed. 43, 6479 (2004)
C12A7 mayenit

## Slide 36: Surface System
periodic among x-y plane while not along z
surface geometric (reconstruction)structure
electronic and magnetic structure
chemical processes on surface
interface of solid-solid, solid-gas and solid-liquid
simulation of spectroscopy, such as STM, IR, XPS etc

## Slide 40: Band Decomposition
LDIPOL = .TRUE.
IDIPOL = 1, 2, 3, 4
LPARD = .TRUE.
IBAND = 20 21 22 23 partial charge density for bands
EINT = E1, E2, if only one relative to Ef
NBMODE = >0, 0, 1, -1, -2, -3 (manual)
KPUSE = 1, 2, 3 , 4 k-points used
LSEPB = .TRUE. (PARCHG. nb,.* will be written)
LSEPK = .TRUE. (PARCHG.*.nk will be written)
LVTOT = .TRUE. (LOCPOT will be written, work function)
MAGMOM, NUPDOWN, NELECT

## Slide 41: Chemical Processes
CINEB method in VASP
IMAGES =
ICHAIN = 0
LCLIMB = .TRUE.
SPRING = -5
J. Chem. Phys. 133, 071101 (2010)

## Slide 42: Core Level Shift (CLS)
Icorelevel = 0 / 1 /2 (approx final/ initial /acc. final state)
CLNT = 1,2,3,... according to POSCAR
CLN = 1,2,3... N quantum number
CLL = 1,2,3 (l QN)
CLZ = 1 (number of electrons removed from core)
NELCT = the number of valence electrons
Z+1 approximation
J. Chem. Phys. 131, 244505 (2009)

## Slide 43: Vibrational Frequencies
IBRION = 5
POTIM = 0.02

## Slide 45: Thank you for your attention!